Phifer 18x16 Fiberglass

*Standard mesh 18x16 fiberglass*

This standard fiberglass screen is the mesh applied in most window and doors. Easily fabricated, this high-quality standard mesh is the preferred insect screening in the fenestration industry.

We carry only Phifer Incorporated Standard Mesh 18x16 mesh fiberglass insect screen, Ask for Phifer by name.

**Technical Information:**

Mesh: 18x16 Nominal Mesh Fiberglass Insect Screen

Standard Window Screen Mesh
Colors: Charcoal and Silver-Gray
Roll Length: 100' & 600' Select Sizes 300'
Widths: 18"-96"

Yarn Diameter (inch) .010 - .011

Fabric Thickness (inch) .0125

Openness (%) 59

Light Transmission 69%

Burst Strength (psi) 92

Aperture: .0027